PRODUCT  DATA  SHEET

G

###### SL-NT AA1 #2

NON-TOXIC GREASE

PRODUCT  DESCRIPTION

SL-NT-AA1 is an edible synthetic, non-toxic, water white, tasteless, and odorless grease.  It is approved by NSF and is included in their list of chemical compounds for use in machinery where there might be direct contact or contamination of the food with the lubricant. It is made from U.S.P. fluids treated with synthetic compounds and other ingredients that are safe to ingest. It is the answer to the food, beverage and pharmaceutical industries and those directly or indirectly serving these industries.

TYPICAL  CHARACTERISTICS

Machinery handling food and allied products are particularly difficult to properly lubricate because of the limitation on materials that are acceptable. The high heat encountered in these, together with the large volumes of water for cleaning, make lubricant retention in the bearings and other parts of these machines difficult.  By using SL-NT-AA1 grease this problem is kept to a minimum.  The grease is waterproof and therefore, will not wash out of a bearing at operating temperatures of 260˚C (500˚F).  SL-NT-AA1 grease has a useful temperature range of -40˚C (-40˚F) to 232˚C (450˚F).

NLGI Grade		2					ASTM D-1092

Worked Penetration		265-295					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-2					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

Water Washout		1.4					ASTM D-1264

Extreme Pressure		20+ (45)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.7mm					ASTM D-2266

Food Grade Status		H1					NSF

NSF Registration		133583

Appearance 		Clear, Transparent

PIN #		                                  	06510

TO ORDER or FOR ADDITIONAL INFORMATION