PRODUCT  DATA  SHEET

G

###### S-ATF

AUTOMATIC

TRANSMISSION FLUID

PRODUCT  DESCRIPTION

Sentinel’s S-ATF is a multi-purpose synthetic DEXRON® III / MERCON® universal multi-functional fluid for automatic and power lift transmissions for all industrial and mobile systems.

S-ATF keeps transmissions operating cooler and smoother, reduces drag for improved fuel economy and increases service life many times over petroleum fluids.

S-ATF enhances performance in severe and cold weather service.  Its synthetic composition and low temperature fluidity offer superior wear resistance, as well as torque converter and equipment protection in cold starting situations.

Dexron®III is a registered trade name of General Motors Corporation.

Mercon® is a registered trade name of Ford Motor Company.

TYPICAL  CHARACTERISTICS

ISO Viscosity Grade	  32   		  			ASTM D-   2422

Viscosity cSt    @ 100C			 	 7.1                                                  	ASTM D-     445

@   40C	                   30.8	                     		ASTM D-     445

Viscosity Index  	196	                    	 	ASTM D-   2270

Pour Point C (F)	                                             -50(-46)		 		ASTM D-       97

Flash Point C (F)                                                   220(428)		                 		ASTM D-       92

Fire point C (F)                                                     242(468)	                    		ASTM D-       92

Foam Sequence I, II, III				    Pass		                               		ASTM D-     892

Demulsibility 82C 			      40/40/0 (15)		                               		ASTM D-   1401

Color Observed                                                                Red

PIN #		                                                               08170

TO ORDER or FOR ADDITIONAL INFORMATION