PRODUCT  DATA  SHEET

###### SENTISHIELD™

###### 4000

###### HIGH PERFORMANCE

HYBRID LUBRICANT

PRODUCT  DESCRIPTION

Sentinel’s SENTISHIELDTM 4000 is a synthetic, heavy duty, extreme pressure, lubricant formulated to meet the severe lubrication demands of the Agricultural, Construction, Forestry, Mining, Railroads, Rock and Quarry Industry.

Sentinel has a long established commitment to develop high performance lubricants while maximizing environmentally friendly, high viscosity index, synthetic base stock for its exceptional physical and chemical stability, and exceptional serviceability over a wide range of temperatures.

TYPICAL  CHARACTERISTICS

SENTISHIELDTM 4000 is additionally compounded to provide superior adhesive film forming characteristics.  This adhesive film forming characteristics allows Sentishield to resists “squeeze out” and to cling tenaciously. SENTISHIELD4000 will support loads up to 500,000 PSI. It exhibits the tenacity and retention characteristics and load carrying capability.

SENTISHIELDTM 4000 is a remarkable hybrid lubricant that provides year round pumpability without the use of chlorinated solvents or heavy metals, and passes the new EPA Toxicity Characteristic Leaching Procedure (TCLP) Test.

AGMA Lubricant Number	13EP+

U.S. Steel 224 Specification	Pass

AGMA 250.04 EP Specification	Pass

Viscosity cSt @ 100C	4000					ASTM D-  445

Viscosity Index	122					ASTM D-2270

Pour Point C (F)	+2 (+35)					ASTM D-    97

Flash Point C (C)	185C (365F)					ASTM D-    92

Fire Point    	307C (585F)					ASTM D-    92

Foam Sequence I, II, III	Pass					ASTM D-  892

Four Ball, EP, Weld Point, kg	800					ASTM D-2783

Load Wear Index, kg	160

Copper Corrosion, 121C (250F) 3 hours	1a					ASTM D-  130

Rust Test	Pass					ASTM D-665AB

FZG, Spur Gear Test, Pass Load Stage	13+					ASTM D-5182

Timken EP, OK Load Kg (lbs)	50 (110)					ASTM D-2782

USDA Rating	H-2

Appearance	Dark Metallic

PIN#						      07400

TO ORDER or FOR ADDITIONAL INFORMATION