PRODUCT  DATA  SHEET

G

###### D-MOIST “S”

DEMOISTURANT

PRODUCT  DESCRIPTION

Displaces moisture – Excellent for use on any equipment that is moisture sensitive such as internal combustion engines, high voltage wiring, distributors, electrical switches, starters, motors, generators, alternators, relays and surfaces that may become conductive.  Superb for use on marine engines and ignition systems.

Stops Rust – Excellent for use on molds, tools, parts, assemblies and new machine metal in indoor storage.  Resistance is provided against acid fumes and salt spray.  A good barrier is created against humidity flash rust and provides up to two years indoor storage without corrosion (unwrapped 6-12 months).

Penetrates – Quickly wicks into free parts locked or frozen by rust, scale, gum, grease, paint and other binding residue.  Easy to use, neat clean and very effective in penetrating threaded fasteners and pins, sleeves, hinges, press fits and many other applications.  Superior in function to CRC and WD-40!

Lubricates – Contains an inhibited oil lubricant suitable for many light duty lubrication uses.  May be used on nut, bolts, pins, shafts, bearings, latches, locks, or the assembly and disassembly of equipment and engines, springs, shackles, light duty sleeve bearings, plastics, wheel lugs, brake hardware, roller chain, chain saws and threaded take-ups.

DIRECTIONS: Shake can well before use.  Can temperature should be 18˚C (65˚F) or warmer. (WARNING:  Never use direct heat to warm aerosol cans!  Only warm water should be used!) For pin-point control, remove spray tip and insert plastic extended tube.  Replace spray tip with a twisting motion, taking care not to spray into face.

Sentinel’s “S” line of spray lubricants are non-ozone depleting products specially formulated for industry.

Sentinel’s “S” line contains no CFC’s, HCFC’s, Methyl chloroform, or any other material known to affect the stratospheric ozone.

TYPICAL  CHARACTERISTICS

Appearance							Light Straw

Film Thickness, mils							            0.13

5% Salt Spray, hours to fail								38

Flash Point of Wet Film, ˚C (˚F)						                > 38 (100)

Flash Point of Dry Film, ˚C (˚F)							  >150(300)

Electrical Conductivity						         Nonconductive

Specific Gravity, g/cc @ 60/60 ˚F							           0.84 Weight, lbs./gal @ 70 ˚F							             7.0

USDA Classification							            H-2

Net Weight per 20oz Aerosol Can	                                                                                             15 oz. (425g)

PIN #					            	                       01042

TO ORDER  or  FOR ADDITIONAL INFORMATION