PRODUCT  DATA  SHEET

###### SL WR WHITE “S”

WHITE WATERPROOF

GREASE

PRODUCT  DESCRIPTION

SL WR “S” White Grease is an outstanding grease for every phase of lubrication including (but not limited to) in the presence of water steam, most acids, or salts.  There is little or no washout, breakdown, or emulsification when subjected to high temperatures.

SL WR “S” White Grease is formulated with materials acceptable to FDA and USDA for use with food handling and food products.  It shrugs off beer, alcohol, beverages, salt, starches, jellies, sugar and flour.  Even the cleaning chemicals used in food plants have little effect on its lubricating properties.  It is recommended for all sides, cams, bearings, and all types of mechanical equipment especially those subjected to water conditions and/or high temperature.

Because of the foregoing and its white color, SL WR “S” White Grease is highly recommended for food plants, dairies, meat packing houses, bakeries, pharmaceutical plants, hospitals, textile plants, etc.

TYPICAL  CHARACTERISTICS

DIRECTIONS:  Shake can well before use. Can temperature should be 18˚C (65˚F) or warmer.  (WARNING:  Never use direct heat to warm aerosol cans! Only warm water should be used!) Insert plastic extender tube for pin point application.  Apply liberally to area to be lubricated.  Wipe off excess.

Sentinel’s “S” line of spray lubricants are non-ozone depleting products specially formulated for industry.

Sentinel’s “S” line contains no CFC’s, HCFC’s, Methyl chloroform, or any other material known to affect the stratospheric ozone.

NLGI Grade	2					        ASTM D-1092

Worked Penetration	265-295					        ASTM D-  217

Dropping Point	None					        ASTM D-2265

Oxidation Stability	-1					        ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative	1a					        ASTM D-1743

No Stain

Water Washout	.5  					        ASTM D-1264

Extreme Pressure	34+ (75)					        ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	0.6mm					        ASTM D-2266

Solids	Zinc Oxide

Appearance	White Opaque Tacky

NSF Registration	152554						H-1

Net Weight per 20oz Aerosol Can	13 oz. (369g)

TO ORDER or FOR ADDITIONAL INFORMATION

PIN #							01015