PRODUCT  DATA  SHEET

###### SLOG “S”

OPEN GEAR COMPOUND

PRODUCT  DESCRIPTION

Sentinel SL-OG “S” is a unique synthetic metallic compound designed for general purpose open gear lubrication.  It has a high tacky content that prevents it from slinging out even at high RPM’s.  It is especially formulated to stay on exposed parts of gears, resisting extreme pressures from close moving parts.  SL-OG “S” has a thermal range of from -40°C to 232°C (-40°F to 450°F) and an E.P. rating in excess of 150,000 P.S.I.

Sentinel SL-OG “S” has metallic particles incorporated into its synthetic carrier making it bronze in color and giving it greater plating action.  It can even be applied while equipment is running.

TYPICAL  CHARACTERISTICS

DIRECTIONS:  Shake can well before use. Can temperature should be 18˚C (65˚F) or warmer.  (WARNING:  Never use direct heat to warm aerosol cans! Only warm water should be used!)  Apply liberally to area to be lubricated.  Wipe off excess.

Sentinel’s “S” line of spray lubricants are non-ozone depleting products specially formulated for industry.

Sentinel’s “S” line contains no CFC’s, HCFC’s, Methyl chloroform, or any other material known to affect the stratospheric ozone.

NLGI Grade	1					        ASTM D-1092

Worked Penetration	310-340					        ASTM D-  217

Dropping Point	None					        ASTM D-2265

Oxidation Stability	-1					        ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative	1a					        ASTM D-1743

No Stain

Water Washout	1.2					        ASTM D-1264

Extreme Pressure	45+ (100)					        ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.7mm					        ASTM D-2266

Solids	Copper/Bronze

Appearance	Gold Metallic Tacky

USDA Classification	H-2

Net Weight per 20oz Aerosol Can	14.5oz. (411g)

PIN #			            01013

TO ORDER or FOR ADDITIONAL INFORMATION