PRODUCT  DATA  SHEET

G

###### S-NT CO Series

NON-TOXIC

COMPRESSOR FLUID

PRODUCT  DESCRIPTION

The increased use of air compressors, not only in industrial plants in general but also in food-processing plants, has created a need for the development of new extended-life lubricants, including those meeting FDA and NSF requirements for incidental food contact.

This led to the development of Sentinel’s® S-NT-CO Series, a new synthetic compressor lubricant/coolant developed from polyalphaolefin (PAO) based fluids.

TYPICAL  CHARACTERISTICS

Tests demonstrated that Sentinel’s® S-NT-CO Series synthetic fluid provided several advantages including good compatibility with the components in standard compressor systems and low foaming properties.  It was also found to have excellent water separation and low water absorption as compared to diester fluids.

S-NT-CO Series meets all the FDA requirements for qualification as a white mineral oil (FDA Regulation 21 CFR 172.878) and means that the fluid maybe used in lubricants for incidental contact as a candidate for NSF rating H-1 for incidental food contact in meat and poultry plants.  The additives used in formulating S-NT-CO also meet all the under Regulation 21 CFR 178.3570.

S-NT-CO10   S-NT-CO10/20  S-NT-CO20   S-NT-CO30   S-NT-CO40

ISO Viscosity Grade		32	46	                      68		                  100	             150        	ASTM D-1092

SAE Viscosity Number 		10	                     10W20                    20	                     30                      40      	 	  	SAE J- 300

Viscosity cSt @100°C	6	 8	                      10	                     14                      18         	ASTM D-  445

@ 40°C	                         32	46	                      68	                     95                     145

Viscosity Index   	                        135                           146                     136                    151                    155        	ASTM D-2270

Pour Point °C (°F)		-60 (-76)                -54 (-65)             -51 (-60)             -51(-60)             -51(-60)    	ASTM D-    97

Flash Point °C (°F)		240 (464)              243 (470)            250 (482)           266 (510)           270(518)   	ASTM D-    92

Foam Sequence I, II, III	    ----------------------------------------  Nil  --------------------------------------         	ASTM D-  892

Four Ball Wear, mm

41 kg, 1200 rpm, 75°C (1 hr)	    ----------------------------------------  0.5 ---------------------------------------		ASTM D-2266

Demulsibility 54.4°C (130°F)	------------------------------------ 40/40/0(15) ----------------------------------

Copper Corrosion 121°C (250°F)		----------------------------------------- 1a -----------------------------------------         	ASTM D-  130

Conradson Carbon Residue %	---------------------------------------- 0.02 ---------------------------------------         	ASTM D-  189

Auto ignition Temperature °C (°F)	------------------------------------- 400 (750) ------------------------------------	    ASTM D-2155

Oxidation Test, hrs	                       4000+                     4000+                 4000+                 8000+	            8000+         ASTM D-  943

Food Grade Status		----------------------------------------  H-1 -----------------------------------------	        NSF

NSF Registration	                      137207                    137208               137209               137210             137211

PIN#                                                14500                      14503                 14505	              14510               14515

TO ORDER or FOR ADDITIONAL INFORMATION