PRODUCT  DATA  SHEET

G

###### S-NT-ALO

###### ISO-46

NON-TOXIC AIRLINE LUBRICANT

PRODUCT  DESCRIPTION

\

Sentinel’s S-NT-ALO ISO 46 is a non-toxic, water white, tasteless, clean, ashless, residue free fluid that cleans as it lubricates to maintain air-flow free from blockage while assuring maximum “wetting” action of all metallic surfaces for reducing wear, tear, and deterioration of expensive equipment.

Sentinel’s S-NT-ALO ISO 46 is an exclusive formulation designed for the lubrication of airlines.  Sentinel incorporates special corrosion additives to eliminate oxidation and rust within the tools.

TYPICAL  CHARACTERISTICS

S-NT-ALO ISO 46 meets all the FDA requirements for qualification as a white mineral oil (FDA Regulation 21 CFR 172.878) and means that the fluid maybe used in lubricants for incidental contact with food as specified in 21 CFR 178.3570.  This regulation qualifies a lubricant as a candidate for NSF rating H-1 for incidental food contact in meat and poultry plants.  The additives used in formulating S-NT-ALO ISO 46 also meet all the requirement under Regulation 21 CFR 178.3570.

ISO Viscosity Grade	46					ASTM D-2422

Viscosity cSt @ 100˚C	7.9					ASTM D-  445

@   40˚C	46

Viscosity Index        	134					ASTM D-2270

Pour Point ˚C (˚F)	-47 (-53)					ASTM D-    97

Flash Point ˚C (˚F)	237 (459)					ASTM D-    92

Foam Sequence I, II, III	Pass					ASTM D-  892

Demulsibility, 82˚C	40/40/0 (30)					ASTM D-1401

Copper Corrosion

121˚C (250˚F), 3 hrs.	1a					ASTM D-  130

Rust Test	Pass					ASTM D-  665 A & B

Food Grade Status	H1					NSF

NSF Registration	140304

Appearance     	Clear

PIN #						08125

TO ORDER or FOR ADDITIONAL INFORMATION