PRODUCT  DATA  SHEET

###### SG-HT Series

HIGH TEMPERATURE

GREASES

PRODUCT  DESCRIPTION

Sentinel’s High Temperature Bearing Greases are composed of highly refined, synthetically fortified fluids compounded with various metallics in sub micron particles in a colloidal suspension, and then formed into solid grease with the finest saponifiers.

Sentinel’s HT Greases are stable to shear and have excellent resistance to water and moisture.

Sentinel’s High Temperature Greases are compounded to provide excellent lubrication and wear protection under heavy loads along with excellent retention and resistance high temperature degradation.  They will not form hard carbon deposits and will eliminate rust and corrosion. Sentinel’s High Temperature Greases are multi-functional, and are recommended for almost any type of oven of high temperature application, such as tenter frames, lithographed or enameled metal baking ovens, etc.

TYPICAL CHARACTERISTICS

SG 400 HT               SG 500 HT              SG 600 HT           SG 700 HT

NLGI Grade		  		      2			      2			   2				  2	ASTM D-1092

Worked Penetration		      265-295		     265-295		    265-295		    265-295	ASTM D-  217

Dropping Point			       None	      None	     None		  None	ASTM D-2265

Oxidation Stability		      -1	      -1	    -1		   -1	ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		        1a	      1a	    1a			    1a	ASTM D-1743

Water Washout			       1.2		     1.2	    1.2		   1.2	ASTM D-1264

Extreme Pressure		     36+ (80)	    36+ (80)	   36+ (80)	  36+ (80)	ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		      .5mm	     .5mm	   .5mm	  .5mm	ASTM D-2266

Solids		      MoS2	       MoS2	     MoS2	    MoS2

USDA Rating		       H-2	      H-2		   H-2		  H-2

Appearance Visual		     Amber	        Red			 Dark Red			   Dark

Smooth	   Smooth	  Smooth	 Metallic

PIN #		     05003	     05013	   05023	    05033

TO ORDER or FOR ADDITIONAL INFORMATION