PRODUCT  DATA  SHEET

G

###### SL-HRPM

HIGH SPEED

BEARING GREASE

PRODUCT  DESCRIPTION

SL-HRPM is the industry’s finest, field proven, synthetic high speed bearing grease.

SL-HRPM is designed for multi-use plant wide application for use in all bearing speeds.  In most plant operations, this grease covers the entire range.  It has superior high temperature oxidation and thermal stability, enabling long lubricant life and reducing maintenance frequency.

TYPICAL CHARACTERISTICS

SL-HRPM sharply reduces inventories and lubricant costs.  Lubrication intervals are extended resulting in less grease consumption, less downtime, and lowered maintenance cost.  It provides superior lubrication protection, helping to extend equipment life.

NLGI Grade			2					ASTM D-1092

Worked Penetration		265-295					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-1					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

Water Washout		.9					ASTM D-1264

Extreme Pressure		36+ (80)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.5mm					ASTM D-2266

USDA Rating		H-2

Appearance 		Blue Smooth

PIN #		                                                        03450

TO ORDER or FOR ADDITIONAL INFORMATION