PRODUCT  DATA  SHEET

G

SL-GRAPH

GR # 2

###### GRAPHITE GREASE

PRODUCT  DESCRIPTION

Sentinel’s SL-Graph GR #2 is an all-purpose synthetic base grease formulated with a high quality powder. SL-GRAPH GR #2 provides maximum lubrication through a wide temperature, pressure and speed variation.

SL-GRAPH GR #2 is fortified with EP additives, rust and corrosion inhibitors.

TYPICAL  CHARACTERISTICS

SL-GRAPH GR #2 will not carbonize, char, freeze or run out of bearing.  It reduces wear, prevents seizing and galling, and lowers the coefficient of friction.  It also increases bearing life and reduces maintenance power consumption.

SL-GRAPH #2 is recommended for all greasing applications, either by hand or grease gun.

NLGI Grade			2					ASTM D-1092

Worked Penetration		265-295					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-1					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

Water Washout		.9					ASTM D-1264

Extreme Pressure		36+ (80)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.5mm					ASTM D-2266

Solids      		Graphite

Appearance 		Dark Metallic

PIN #		                                                      03415

TO ORDER or FOR ADDITIONAL INFORMATION