PRODUCT  DATA  SHEET

G

###### SL-123R

A TRUE ALL PURPOSE

MULTI-GRADE GREASE

PRODUCT  DESCRIPTION

SL 123 R is the industries’ finest, field proven, heavy duty, high temperature and synthetic multi-purpose grease. SL123 R is designed for multi-use plant wide application for use in plain bearings, anti-friction bearings, and grease-lubricated gears and couplings.  SL 123 R has superior high temperature oxidation and thermal stability enabling long lubricant life.  Furthermore, the newer homogenization process stabilizes the base grease compound, which improves the lubricating ability at high temperatures and enables use over a wide temperature range.

SL 123 R cannot be extruded from lubricating interface areas by sudden shock loads and extreme pressures.  SL 123 R has been tested and has been proven to exceed 36+ kilos (80 lbs.)  Timken for extreme pressure loading.  It extends service and reduces maintenance frequency. SL 123 R has excellent inherent rust and corrosion inhibitors, and is highly recommended for sealed life bearings and long lasting greasing.

TYPICAL  CHARACTERISTICS

SL 123 R consolidates all grease requirements; it sharply reduces inventories and lubrication costs.  Moreover, lubrication errors that can occur when using numerous types of greases are avoided due to its general-purpose versatility and high temperature properties. Lubrication intervals are extended resulting in less grease consumption, less downtime, and lowered maintenance cost.  It provides superior lubrication, helping to extend equipment life.

SL 123 R will plate out a metallic film onto all metal working parts immediately and requires no burnishing period to accomplish this, thereby exhibiting an instant anti-seize property.  SL 123 R is recommended for all greasing applications either by hand, grease gun, central lube system, etc.

NLGI Grade         	1-2-3 					ASTM D-1092

Worked Penetration	265-295					ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability, Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative, No Stain	1a					ASTM D-1743

Water Washout	.5					ASTM D-1264

Extreme Pressure, Timken OK Load Kg (Lb)	36+ (80)					ASTM D-2509

Four Ball Wear	.5 mm					ASTM D-2266

Solids	MoS2

Food Grade Status	H2					NSF

NSF Registration	137134

Appearance	Red Smooth

PIN #		                                                            03159

TO ORDER OR FOR ADDITIONAL INFORMATION