PRODUCT  DATA  SHEET

###### SL-WPG

WATERPROOF

GREASE

PRODUCT  DESCRIPTION

SL-WPG is an outstanding synthetic lubricating grease for every phase of lubrication.  Its performance is exceptional in the presence of water though definitely not limited to this type of application.  It cannot be washed out, even when subjected to high rpm, boiling waters and extreme temperatures under 204°C (400°F).

TYPICAL  CHARACTERISTICS

SL-WPG has superior tenacity and is heavy-bodied; it clings tenaciously to metal surfaces.  It will not pound out, sling out, dissolve out or melt out.

SL-WPG is recommended for all types of bearings, slides, cams, and in all types of mechanical equipment subjected to water and or salt conditions at any temperature range from -28°C (-20°F) to 227°C (440°F).

NLGI Grade         	2 					ASTM D-1092

Worked Penetration	265-295					ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability

Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative	1a					ASTM D-1743

No Stain

Water Washout	.4					ASTM D-1264

Extreme Pressure	34+ (75)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.6 mm					ASTM D-2266

Solids	MoS2

Food Grade Status	H2					NSF

NSF Registration	137132

Appearance	Blue Green Stringy

PIN #		                                                    03090

TO ORDER or FOR ADDITIONAL INFORMATION