PRODUCT  DATA  SHEET

G

###### SLM-2

MULTI-USE

WATERPROOF GREASE

PRODUCT  DESCRIPTION

SLM-2 is a superior synthetic grease. This grease has been formulated with molybdenum disulfide to obtain the optimum in anti-wear and extreme pressure qualities. It is practically neutral in pH and is extremely water resistant. It is not affected by water (hot or cold), steam or most acids and salts.

When heavy bearing loads are re-encountered by SLM-2 and boundary lubrication occurs, the molybdenum disulfide is activated to form a continuous monomolecular film. This film on metal surfaces resists metal to metal contact and reduces wear in “contact lubrication.”

TYPICAL  CHARACTERISTICS

SLM-2 also lubricates better under hydrodynamic lubrication conditions because of its exceptional mechanical stability.

NLGI Grade         	2					ASTM D-1092

Worked Penetration	265-295	 				ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability

Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative	1a					ASTM D-1743

No Stain

Water Washout	0.7					ASTM D-1264

Extreme Pressure	45+ (100)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.4 mm					ASTM D-2266

Solids	MoS2

USDA Rating	H-2

Appearance        	Dark Metallic

PIN #		                                                          03039

TO ORDER or FOR ADDITIONAL INFORMATION