PRODUCT  DATA  SHEET

G

###### SLM-1

MULTI-USE

WATERPROOF GREASE

PRODUCT  DESCRIPTION

SLM-1 is a superior synthetic grease.  This grease has been formulated with molybdenum disulfide to obtain the optimum in anti-wear and extreme pressure qualities.  It is practically neutral in pH and is extremely water-resistant.  Therefore, it is not affected by water (hot or cold), steam or most acids or salts.

TYPICAL  CHARACTERISTICS

When heavy bearing loads are reencountered by SLM-1 and boundary lubrication occurs, the molybdenum disulfide is activated to form a continuous monomolecular film.  This film on metal surfaces resists metal to metal contact and reduces wear in “contact lubrication.”

SLM-1 lubricates better under hydrodynamic lubrication conditions because of its exceptional mechanical stability.

NLGI Grade         	1					ASTM D-1092

Worked Penetration	310-340					ASTM D-  217

Dropping Point	None  					ASTM D-2265

Oxidation Stability

Psi drop @ 100 hrs	-1					ASTM D-  942

Rust Preventative	1a					ASTM D-1743

No Stain

Water Washout	.7					ASTM D-1264

Extreme Pressure	45+ (100)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.4 mm					ASTM D-2266

Solids	MoS2

USDA Rating	H-2

Appearance        	Dark Metallic

PIN #		                                                              03037

TO ORDER or FOR ADDITIONAL INFORMATION