PRODUCT  DATA  SHEET

G

###### SL-NT OGG

NON-TOXIC

OPEN GEAR COMPOUND

PRODUCT  DESCRIPTION

Sentinel’s SL-NT-OGG is a unique synthetic, non-toxic, water white, tasteless, odorless grease designed for general purpose open gear lubrication.  It has a high tacky content that prevents it from slinging out even at high RPM’s.  It is specifically formulated to stay on exposed and open gears, resisting extreme temperatures as well as extreme pressures from close moving parts.

Shock and noise are reduced.  Uneven wear is prevented.  It can even be applied while equipment is running.

TYPICAL  CHARACTERISTICS

Unlike petroleum based gear lubes, SL-NT-OGG is not susceptible to water and is not affected by heat, cold, or extreme pressures.  It will not harden in cold weather, or melt out in warm weather.

SL-NT-OGG complies with FDA regulation Title 21, CFR 178.3570 and NSF H-1 rating.  SL-NT-OGG may be used in equipment that may come in contact with food for incidental contact.

NLGI Grade			1					ASTM D-1092

Worked Penetration		310-340					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-2					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

Water Washout		2.0					ASTM D-1264

Extreme Pressure		25+ (55)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.7mm					ASTM D-2266

Food Grade Status		H1					NSF

NSF Registration		140317

Appearance 		Clear, Tacky, Smooth

PIN #		                                            	06550

TO ORDER or FOR ADDITIONAL INFORMATION