PRODUCT  DATA  SHEET

G

###### SL-NT C

NON-TOXIC

CRYOGENIC GREASE

PRODUCT  DESCRIPTION

SL-NT-C is the newest member of the well-known Sentinel family of food grade lubricants.

SL-NT-C is a multi-purpose synthetic, extreme low temperature, non-toxic, water white, tasteless, and odorless grease.  SL-NT-C is a synthetically thickened grease which employs an extremely low viscosity Polyalphaolefin (PAO) based fluid.

Its low temperature torque characteristic at -73°C (-100°F) is a functional benefit that conventional greases cannot achieve.

SL-NT-C complies with FDA regulations Title 21, CFR 178.3570 and is registered with NSF for use in food processing plants.  SL-NT-C has received an H-1 rating.

TYPICAL  CHARACTERISTICS

NLGI Grade			1½ 					ASTM D-1092

Worked Penetration		290-315					ASTM D-  217

Dropping Point		None 					ASTM D-2265

Oxidation Stability 		-2					ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative		1a					ASTM D-1743

Water Washout		2.0					ASTM D-1264

Extreme Pressure		20+ (45)					ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear		.7mm					ASTM D-2266

Food Grade Status		H1					NSF

NSF Registration		140316

Appearance 		Clear, Smooth

PIN #		                                              06540

TO ORDER or FOR ADDITIONAL INFORMATION