PRODUCT  DATA  SHEET

G

###### RUST-AWAY

RUST REMOVER

PRODUCT  DESCRIPTION

Rust-Away is a blend of acids that removes rust, welding scale, heat marks, light oil and shop oil from carbon steel and iron.  It is also effective for removing light oxide and tarnish from copper or copper alloys (brass, bronze and monel).

TYPICAL  CHARACTERISTICS

It produces a hard thin surface conditioning on steel that serves as an excellent base for paint, or other organic coatings.

Physical Appearance						Clear Orange Liquid

Odor             	       						          None

Viscosity     	       					   	      10 CPS.

PH @ 77°F           	  					       	             1.0

Flash Point							          None

Shelf Life 							 1 year plus

Specific Gravity @ 77°F							           1.14

Weight per Gallon @ 77°F 							           9.47

Biodegradable         							           Yes

Solvents							         None

Toxicity					    Contains a Blend of Acids

POISON – MAY CAUSE SEVERE BURNS

PIN #							       02001

TO ORDER or FOR ADDITIONAL INFORMATION