PRODUCT  DATA  SHEET

G

###### S-WGO Series

WORM GEAR OIL

PRODUCT  DESCRIPTION

S-WGO Series is a synthetic, multi-purpose, specially compounded molybdenum disulfide worm gear lubricant, formulated to protect moderate to heavily loaded industrial gears and bearings.  S-WGO Series provides excellent anti-wear and load carrying capability, as well as strong rust inhibition, yellow metal protection, and demulsibility performance.

S-WGO Series exceeds the FZG load carrying requirements and Four Ball Wear specification of all existing gear lubricants.

TYPICAL  CHARACTERISTICS

S-WGO Series provides improved high temperature stability and cleanliness, excellent low temperature fluidity and better overall lubricity.  These characteristics help reduce costs by extending service intervals and reducing power consumption.

S-WGO Series is suitable for use in spur, herringbone, helical, bevel, as well as all types of worm gearing.

ISO Viscosity Grade                150                  220                 320               460          	 680	         1000      	         ASTM D-2422

AGMA Lubricant Grade            4                     5	              6 	                 7 		   8	           8A	                        SAE J-      300

Viscosity cSt @ 100˚C            17.5                22.8	            29.1	               37.2             47.9    	          58.5	         ASTM D-  445

@   40˚C            150                  220       	           320	               460	 	  680	         1000

Viscosity Index                       120                 127	             124	               123		  121	          113	         ASTM D-2270

Pour Point ˚C (˚F)               -40(-40)          -37(-30)	         -34(-30)         -29(-20) 	   -26(-15)	        -26(-15)	         ASTM D-    97

Flash Point ˚C (˚F)               243(470)        240(475)	         243(470)       241(465)	   238(460)         290(554)	         ASTM D-    92

Foam Sequence I, II, III      ----------------------------------------------------- PASS------------------------------------------                ASTM D-  892

Demulsibility 82˚C              --------------------------------------------------40-40-0 (30)--------------------------------------              ASTM D-1401

Four Ball Wear, mm

40 kg, 1200 rpm, 75˚C(1 hr)   .40	          .40	            .40                .40                .40                  .35                        ASTM D-2266

Copper Corrosion

121˚C (250˚F), 3 hrs.     -------------------------------------------------------1b---------------------------------------------------  	       ASTM D-  130

Rust Test                             -----------------------------------------------------PASS----------------------------------------------     ASTM D-665A&B

Gear Test, FZG, SPUR, Stage Pass ----------------------------------------------12+------------------------------------------

Color                                  ----------------------------------------------------Dark Metallic----------------------------------

PIN #                                   47233              47238            47246            47250              47254            47267

TO ORDER or FOR ADDITIONAL INFORMATION