PRODUCT  DATA  SHEET

G

###### TTF-1000

###### TTF-1000 XND

TENTERFRAME

PRODUCT  DESCRIPTION

Sentinel’s TTF-1000 blended synthetic lubricant capable of lubricating at high temperatures without depositing any residue, such as carbon, varnish or sludge.  TTF-1000 is compounded with a blend of specifically engineered lubricating solids for added protection against wear.

Sentinel’s TTF-1000 is a new base oil which was designed specifically for tenter frame applications over a wide temperature range.  Recommended for use where low corrosion of both ferrous and non-ferrous metals at high temperatures is considered to be of primary importance.

TYPICAL  CHARACTERISTICS

Sentinel’s TTF-1000 applications include lithographing ovens, plywood drying ovens, tenter frames in textile mills, lens and glass forming equipment in glass plants, annealing furnaces, paint and ceramic curing ovens, and others where chains and bearings are operating at high temperatures.

TTF-1000 can be applied to chains with a drip oiler, brushes or wheel, by emerging in a bath, or by spray.

TTF-1000 XND is for applications where oil dripping is not acceptable or where superior retention of the oil is desired.

ISO Viscosity Grade	           			220					ASTM D-2422

Viscosity cSt @ 100˚C        				23	 					ASTM D-  445

@  40˚C				220

Viscosity Index				128				ASTM D-2270

Pour Point ˚C (˚F)   	       		-29 (-20)			ASTM D-    97

Flash Point ˚C (˚F)             				290 (554)                    	ASTM D-    92

Fire Point ˚C (˚F) 	      				308 (586)				ASTM D-    92

Foam Sequence I, II, III				Pass					ASTM D-  892

Demulsibility, 82˚C					40 / 40 / 0 (15)			ASTM D-1401

Four Ball Wear, mm

40kg, 1200 rpm, 1 hr., 75˚C  		.41				ASTM D-2266

Copper Corrosion, 121˚C  (250˚F) 3 hrs	1a			ASTM D-  130

Rust Test			Pass				ASTMD-665A&B

USDA Classification             		H-2

PIN #	          		TTF-1000                                                                          16106

PIN#			TTF-1000XND			     16107

TO ORDER or FOR ADDITIONAL INFORMATION

PIN#		TT