PRODUCT  DATA  SHEET

G

###### TTF-500

###### TTF-500M

HIGH TEMPERATURE

TENTER FRAME OIL

PRODUCT  DESCRIPTION

Sentinel’s TTF-500 is a blended synthetic lubricants capable of lubricating at high temperatures without depositing any significant residue, such as carbon, varnish or sludge.

TTF-500 protects against wear and oxidation and dramatically lengthens the service life of the lubricants.  This new high temperature oil was designed specifically for Tenter Frame applications over a wide temperature range.  Recommend for use where low corrosion of both ferrous and non-ferrous metals at high temperature.

TYPICAL  CHARACTERISTICS

TTF 500 can be applied to chains with a drip oiler, brushes or wheel, by immersing in a bath, or by spray.

The special homogenization of the base fluids along 21st Century additive technology enables this product to stay slicker on the chains, therefore keeping the evaporation process evenly distributed thus preventing oil build-up and eliminates smoke.

TTF-500 is also available with Moly (TTF-500M) and XND (TTF-500XND) or a combination of both.

TTF 500				TTF 500M

ISO Viscosity Grade	           	100				100			ASTM D-2422

Viscosity cSt @ 100˚C        	12.4				12.4 		ASTM D-  445

@  40˚C	95				95

Viscosity Index		124				124		ASTM D-2270

Pour Point ˚C (˚F)   	       	 -32 (-25)			-32 (-25)	ASTM D-    97

Flash Point ˚C (˚F)             		257 (495)					257 (495)                    	ASTM D-    92

Fire Point ˚C (˚F) 	      		282 (540)					282 (540)	ASTM D-    92

Foam Sequence I, II, III		Pass					Pass		ASTM D-  892

Demulsibility, 82˚C			40 / 40 / 0 (15)				40 / 40 / 0 (15)	ASTM D-1401

Four Ball Wear, mm

40kg, 1200 rpm, 1 hr., 75˚C  	.41			.40		ASTM D-2266

Copper Corrosion,

121˚C  (250˚F) 3 hrs	1a 			1a		ASTM D-  130

Rust Test		Pass			Pass		ASTMD-665A&B

Color		Amber			Dark Metallic

USDA Classification             	H-2			H-2

PIN #	          	16080		16087

TO ORDER or FOR ADDITIONAL INFORMATION