PRODUCT  DATA  SHEET

G

###### SCO-S	Series

SUPER SYNTHETIC

AIR COMPRESSOR OILS

PRODUCT  DESCRIPTION

Sentinel’s Synthetic Air Compressor Oils (SCO S Series) are polyolester synthetic compounded fluids designed to give long, trouble-free operation of air compressors and vacuum pumps.  They are recommended for all reciprocating, rotary, centrifugal, lobe and screw type air compressors, either stationary or portable.

SCO S Oil Series are recommended for all service conditions from intermittent light load to continuous heavy-duty applications where its superior performance becomes more apparent.

SCO S Oil Series are made from highly refined, chemically stable, high viscosity index base stock, with a compounding including fortified high temperature ashless oxidation inhibitors, preventing gumming, sludge, and resin formation in the valves and working parts of the compressor.

Different from automotive oils approved for compressors and vacuum pumps, these products will not emulsify with water.  They will not foam, and they will not form hard varnishes.

SCO S Oil Series will tremendously reduce maintenance in all air compressors, as well as fire hazards and explosion risks.

SCO S Oil Series will prevent carbon and resin even in the most severe conditions under high temperature, 100% duty cycle, 4 stage compressors.  They will reduce wear and operate cooler because of their superior thermal heat transfer and viscosity stability.  SCO S Oil Series will be consumed less due to their inherently lower evaporation rate and will not be liable to be found in air lines as petroleum oils would.

PRODUCT  ADVANTAGES

Extended drain intervals

Extended oil separator service intervals

Fewer air filter changes

Improved compressor efficiencies

Less downtime

Reduced feed rates

Reduced oil carryover

Reduced vapor pressure

Reduced equipment operational problems

Reduced oil consumption

Reduced maintenance costs

Improved Safety

Eliminates seasonal oil change

Excellent high temperature stability

Improved oxidation stability

Energy conservation

Less oil carryover

Cooler running

TO ORDER or FOR ADDITIONAL INFORMATION

TYPICAL  CHARACTERISTICS

###### SCO-S	Series

SUPER SYNTHETIC

AIR COMPRESSOR OILS

SCO-10S	          SCO-10W20S	       SCO-20S	            SCO-30S	                 SCO-40S                           ASTM METHOD

ISO Viscosity Grade		32		                                  46	                             68	                      100			D-2422

SAE Viscosity Number		10                                                                       20			                  20		         30		                          J-300

Viscosity cSt @ 100°C	   5.4                                10.6                                8.6			                12.4		        17.9		           D-445

@   40°C	  28.2                                 58                               46.4			                66.4                            102		                         D-445

Viscosity Index	  132                                 175                               177			                 188		        194		                         D-2270

Pour Point °C (°F)                          -57(-70)                          -48(-50)                       -54(-65)		             -51(-55)		     -45(-45)		           D-97

Flash Point °C (°F)                         264(505)                        266(510)                      266(510)	             266(510)		     264(505)	                          D-92

Fire Point ˚C (˚F)                            280(535)                        290(554)                      280(550)	             292(555)		     288(550)	                          D-92

Foam Sequence I, II, III                 --------------------------------------------------------     Nil       ----------------------------------------------------------------	D-892

Demulsibility 54.4C (130°F)       -----------------------------------------------------   40/40/0(15)   -------------------------------------------------------------		D-1401

Four Ball Wear, mm 40kg, 1200 rpm, 75°C (1hr)  ------------------------------------      0.5     -----------------------------------------------------------------     		D-2266

Copper Corrosion 121C(250F), 3 hrs  -------------------------------------------------      1a      -----------------------------------------------------------------	D-130

Rust Test                                         -------------------------------------------------------     Pass    -----------------------------------------------------------------	D-665AB

Conradson Carbon Residue %       --------------------------------------------------------    0.08    ----------------------------------------------------------------- 	D-189

Autoignition Temperature °C (°F) ------------------------------------------------------   410(765)  ----------------------------------------------------------------		D-2155

Oxidation Test, hrs		   ------------------------------------------------------     16000+   ----------------------------------------------------------------		D-943

USDA Rating			   --------------------------------------------------------     H-2   ------------------------------------------------------------------

PIN#			14120	14190                        14130                           14140    	        14150

TO ORDER or FOR ADDITIONAL INFORMATION