PRODUCT  DATA  SHEET

G

PRODUCT  DESCRIPTION

###### SCO Series

SYNTHETIC

AIR COMPRESSOR OIL

Sentinel’s Synthetic Air Compressor Oils (SCO Series) are specifically compounded to give long, trouble-free operation of air compressors and vacuum pumps.  They are recommended for all reciprocating, rotary, centrifugal, lobe and screw type air compressors, either stationary or portable.

SCO Oil Series are recommended for all service conditions from intermittent light load to continuous heavy-duty applications where its superior performance becomes more apparent.

PRODUCT ADVANTAGES

SCO Oil Series are made from highly refined, chemically stable, Polyalphaolefin (PAO), high viscosity index base stock, with a compounding including fortified high temperature ashless oxidation inhibitors, preventing gumming, sludge, and resin formation in the valves and working parts of the compressor.

Different from automotive oils approved for compressors and vacuum pumps, these products will not emulsify with water.  They will not foam, and they will not form hard varnishes.

SCO Oil Series will tremendously reduce maintenance in all air compressors, as well as fire hazards and explosion risks.

Extended drain intervals

Extended oil separator service intervals

Fewer air filter changes

Improved compressor efficiencies

Less downtime

Reduced feed rates

Reduced oil carryover

Reduced vapor pressure

Reduced equipment operational problems

Reduced oil consumption

Reduced maintenance costs

Improved Safety

Eliminates seasonal oil change

Excellent high temperature stability

Improved oxidation stability

Energy conservation

Less oil carryover

Cooler running

TO ORDER or FOR ADDITIONAL INFORMATION

###### SCO Series

SYNTHETIC

AIR COMPRESSOR OIL

TYPICAL  CHARACTERISTICS

SCO 10	             SCO 10W 20		   SCO 20	           SCO 30		      SCO 40	     ASTM METHOD

ISO Viscosity Grade		32		46		68	100                               150			D-2422

SAE Viscosity Number		10	20		20			30		          40		           SAE J-300

Viscosity cSt @ 100°C		5.9	7.3		10.6			14		          17		           D-445

@   40°C		30.4	42.3		67.2			95		         142

Viscosity Index		142	136		155			151		         130	           D-2270

Pour Point °C (°F)		-43(-45)	-40(-40)		-40(-40)		-37(-35)		      -35(-30)	           D-97

Flash Point °C (°F)		232(450)	243(470)		243(470)		260(500)	      260(500)	           D-92

Foam Sequence I, II, III               --------------------------------------------------------------------Nil----------------------------------------------------------------                D-892

Demulsibility 54.4C (130°F)      ---------------------------------------------------------------40/40/0(15)----------------------------------------------------------	  D-1401

Four Ball Wear, mm 40kg, 1200 rpm, 75°C (1hr)-------------------------------------------------.5-----------------------------------------------------------------     	  D-2266

Copper Corrosion 121C(250F), 3 hrs -------------------------------------------------------------1a-----------------------------------------------------------------               D-130

Rust Test                                         ------------------------------------------------------------------Pass---------------------------------------------------------------               D-665AB

Conradson Carbon Residue %       -------------------------------------------------------------------.02----------------------------------------------------------------               D-189

Autoignition Temperature °C (°F)------------------------------------------------------------400(750)-----------------------------------------------------------------	           D-2155

Oxidation Test, hrs.		 -------------------------------------------------------------------8000+--------------------------------------------------------------	           D-943

USDA Rating			---------------------------------------------------------------------H-2----------------------------------------------------------------

PIN#			14000	    14085	  14010		14020    		       14030

TO ORDER or FOR ADDITIONAL INFORMATION