PRODUCT  DATA  SHEET

G

###### SC GBO

LOW TEMPERATURE

CRYOGENIC GEAR BOX OIL

PRODUCT  DESCRIPTION

Sentinel’s SC-GBO Blended Synthetic Metallic gear oil is carefully formulated to meet the needs of all types of gear boxes that operate in sub-zero conditions.

SC-GBO’s high film strength and “plating” properties deposit a continuous synthetic metallic lubricating film – not unlike adry film – on all gears and bearings, preventing metal-to metal contact under virtually all conditions, as well as rust and corrosion.

TYPICAL CHARACTERISTICS

This material eliminates costly wear, even on case hardened gears, metal fatigue, break-downs; therefore, parts replacement, repair labor and downtime costs are substantially reduced.

SC-GBO is particularly recommended for equipment that is subject to wide temperature variations, owing to seasonal weather changes, unusual operating conditions, (for example, hydraulic lift trucks that travel between hot and cold locations), and gear boxes of all types that continuously operate in sub-zero/artic – or “deep soak” – conditions.

ISO Viscosity Grade	22					ASTM D-2422

AGMA Lubricant Number 	---

Viscosity cSt @ 100˚C	3.5					ASTM D-  445

@   40˚C	14.4

@  -40˚C	2025

Viscosity Index        	123					ASTM D-2270

Pour Point ˚C (˚F)	-66 (-80)					ASTM D-    97

Flash Point ˚C (˚F)	228(440)					ASTM D-    92

Fire Point ˚C (˚F)	252 (485)					ASTM D-    92

Foam Sequence I, II, III	Pass					ASTM D-  892

Demulsibility 82˚C	40/40/0 (30)					ASTM D-1401

Four Ball Wear, mm 40 kg, 1200 rpm, 75˚C (1hr)	.38					ASTM D-2266

Copper Corrosion 121˚C (250˚F), 3 hrs.	1a					ASTM D-  130

Rust Test	Pass					ASTM D-  665 A & B

FZG, Gear Test, Spur, Stage Pass	12+

Timken OK Load Kg (Lb)	36+ (80)					ASTM D-2509

USDA Rating	H-2

PIN #						13010

TO ORDER or FOR ADDITIONAL INFORMATION