PRODUCT  DATA  SHEET

G

###### DSF 3000

HIGH TEMPERATURE

GREASE

PRODUCT  DESCRIPTION

DSF 3000 is the state of the art in a High Temperature Grease.  It is specifically formulated as a high temperature lubricant to be applied where conventional soap-thickened, or so-called no melt clay-thickened greases will not provide adequate performance.  DSF 3000 High Temperature is a synthetically thickened grease which employs a highly, thermally stable synthetic base oil.  DSF 3000 will not oxidize, as a petroleum base oil/grease will at elevated temperatures.

TYPICAL  CHARACTERISTICS

DSF 3000 High Temperatures Grease is recommended for application where grease lubrication is called for and where continuous temperature exceeds 260˚C (500˚F).  Maximum working temperature for DSF 3000 High Temperature should be considered to be approximately 427˚C (800˚F), however, higher temperature on an intermittent basis are acceptable to the 538˚C (1000˚F) point.

NLGI Grade	1½		                        	                      ASTM D-1092

Worked Penetration	290-315					        ASTM D-  217

Dropping Point	None					        ASTM D-2265

Oxidation Stability	-2					        ASTM D-  942

Psi Drop @ 100 hrs

Rust Preventative	1a					        ASTM D-1743

Water Washout	1.1 					        ASTM D-1264

Extreme Pressure	25+ (50) 					        ASTM D-2509

Timken OK Load Kg (Lb)

Four Ball Wear	.8mm					        ASTM D-2266

Food Grade Status  	H2 rated					        	NSF

NSF Registration  	#137136

Appearance Visual	Blue Smooth

PIN # 				               	              05067

TO ORDER or FOR ADDITIONAL INFORMATION